Section 807 of the Standard Specifications for Highway Construction, Edition of 2003, is hereby amended as follows:

Subsection 807.77(b)(2) is hereby deleted and the following substituted therefore:

(2) Color.  The color of the urethane paint shall match the Federal Standard 595B Color Chip No. X7200, Aluminum color, unless otherwise specified on the plans. (Level of Gloss “X” shall be identified as 1, 2, or 3 finish).  The same level of gloss must be used for all applications of the finish system under the Contract.