## Slide 1: TRC1902: Capillary Pressure Sensor Testing to Identify Curing Regimen in Freshly Placed Concrete Bridge Decks
Samuel Spann, Cameron D. Murray, Ph.D., Micah Hale, Ph.D., P.E.

## Slide 2: Overview
Shrinkage in concrete
CPSS Explanation
Promoting shrinkage cracking
Current progress
Preliminary results
Future work

## Slide 3: Shrinkage in concrete
Extra water is used in concrete mixtures (workability)

## Slide 4: Shrinkage in concrete
When water leaves the concrete, shrinkage happens
Two main types of cracking:
  Plastic shrinkage (before concrete hardens)
  Drying shrinkage (after concrete hardens)

## Slide 5: Shrinkage in concrete
Drying shrinkage
  Regular intervals
  Tend to be deep
Notes: Elm springs road bridge over I49 in Springdale

## Slide 6: Shrinkage in concrete
Plastic shrinkage
  More cosmetic
  Shallow cracks
  Often random patterns
  Occurs before concrete hardens!
https://www.forconstructionpros.com/concrete/equipment-products/article/11487540/plastic-shrinkage-cracking

## Slide 7: Plastic shrinkage
Caused by evaporation of bleed water
Bleed water

## Slide 8: Plastic shrinkage
Rate of evaporation > bleed water rate = plastic shrinkage cracks

## Slide 9: Capillary Pressure Sensor System (CPSS)
Evaporation leads to capillary pressure
  Builds up in concrete surface until the strength < stress
  We can measure these pressures

## Slide 10: Capillary Pressure Sensor System (CPSS)

## Slide 11: Capillary Pressure Sensor System (CPSS)

## Slide 12: Promoting plastic shrinkage cracking
Increased air temperature
Increased concrete temperature
Increased wind speed
Lead to increased rate of evaporation

## Slide 13: Trying to cause cracking
Notes: Unsuccessful January Attempt

## Slide 14: Trying to cause cracking
Warmer temperatures
Restraint
  No restraint = no stress

## Slide 15: Formwork changes

## Slide 16: Next attempt

## Slide 17: Next attempt – successful!

## Slide 18: Current work

## Slide 19: Current work
No curing
Wet burlap + plastic sheeting
Lithium based curing compound
Other compound (white or clear)

## Slide 20: Curing methods
Selected from ARDOT QPL
  WR Meadows 1100 resin based, curing compound (clear)
  WR Meadows 1610 wax based curing compound (white)
  Sinak 1000 lithium cure
Other method
  Wet burlap + plastic sheeting

## Slide 31: Anticipated results
Comparative study of the effectiveness of curing methods
  Data from VWSG and CPSS
Understanding of how to use CPSS
Field trials
Training for ARDOT

## Slide 32: Questions?
Contact:
cdmurray@uark.edu